## Slide 1
Introduction to Inelastic Neutron Scattering and handling powder INS data.
Notes: 1

## Slide 2
Inelastic neutron scattering
Why?
Material properties depend on their structure
But, atoms are not stationary
Dynamics also important → inelastic neutron scattering can measure the dynamics of atom and spins.
Notes: 2
Inelastic neutron scattering measures

## Slide 3
Inelastic neutron scattering
In elastic scattering, need to satisfy Bragg condition
Can be represented in an Ewald construction (sphere)
For inelastic scattering, |ki| ≠ |kf|
Now, have Q = ki – kf which defines the scattering triangle.
ki
kf
G
ki
Ewald’s sphere
ki
kf
G
ki
Q
Notes: 3
Inelastic neutron scattering measures

## Slide 4
The scattering triangle can be mapped directly to the axes of a 3-axis spectrometer
(ki and kf determined by Bragg diffraction from crystals)
Triple Axis Spectrometer
ki
kf
ki
Q
ki
kf
q1
A4
q2
A3
A2
A1
A6
A5

## Slide 5
The scattering triangle can be mapped directly to the axes of a 3-axis spectrometer
(ki and kf determined by Bragg diffraction from crystals)
Rotating crystal effectively rotates the scattering triangle.
Triple Axis Spectrometer
ki
kf
ki
Q
ki
kf
q1
A4
q2
A3
A2
A1
A6
A5

## Slide 6
Powder INS
When we have a powder / polycrystalline sample, we have a random orientation of crystallites:
So the effectively we’re measuring an average over spherical shell of radius |Q|:
ki
kf
ki
Q

## Slide 7
Powder INS
When we have a powder / polycrystalline sample, we have a random orientation of crystallites:
So the effectively we’re measuring an average over spherical shell of radius |Q|:
ki
kf
ki
Q

## Slide 8
Powder INS
When we have a powder / polycrystalline sample, we have a random orientation of crystallites:
So the effectively we’re measuring an average over spherical shell of radius |Q|:
ki
kf
ki
Q

## Slide 9
Powder INS
When we have a powder / polycrystalline sample, we have a random orientation of crystallites:
So the effectively we’re measuring an average over spherical shell of radius |Q|:
ki
kf
ki
Q

## Slide 10
Need a way to define the incident and/or scattered neutron energies (ki or kf ).
At continuous sources, need to use Bragg diffraction from crystals.
At time-of-flight sources,
can use crystals or
mechanical choppers:
Instruments

## Slide 11
At a continuous source (e.g. reactor), with a 3-axis spectrometer, need to define both ki and kf
Instruments
ki
kf
q1
A4
q2
A3
A2
A1
A6
A5

## Slide 12
At time-of-flight sources, only need to define one of ki or kf , the other is determined by the detector position and neutron time-of-flight.
  “Direct geometry”: Fix ki
  “Indirect geometry”: Fix kf
Instruments
Direct geometry
kf
ki
Q
kf

## Slide 13
At time-of-flight sources, only need to define one of ki or kf , the other is determined by the detector position and neutron time-of-flight.
  “Direct geometry”: Fix ki
  “Indirect geometry”: Fix kf
Instruments
Indirect geometry
kf
ki
Q
ki

## Slide 14: MARI
Spec
Ei = 7 meV to 1 eV
922 3He tubes; 3° to 130°
ΔE/Ei = 2.5 - 5%
Direct Geometry Instruments

## Slide 15: MAPS
Spec
Ei = 40 meV to 2 eV
40000 3He PSD elements; 3° to 20° - main bank 20° to 60° - high angle bank
ΔE/Ei = 1 - 5%
Direct Geometry Instruments

## Slide 16: MERLIN
Spec
Ei = 10 meV to 2 eV
π steradians of 3He PSDs
(gapless)
x20 Maps flux
x7 Maps detector coverage
ΔE/Ei = 4 - 6%
Direct Geometry Instruments

## Slide 17: LET
Spec
Ei = 0.5 meV to 20 meV
π steradians of 3He PSDs
(gapless)
Same flux/coverage as Merlin
ΔE/Ei = 0.6 - 3.5%
Direct Geometry Instruments

## Slide 18: Instrument suite
LET
MERLIN
MARI
MAPS
(Flux)
Ei (meV)
Q (Å)
Direct Geometry Instruments

## Slide 19: Around the world
ISIS | LET | MAPS | MERLIN
ILL | IN5 | - | IN4
SNS | CNCS | SEQUOIA | ARCS
J-Parc | Amateras | HRC | 4Seasons
Direct Geometry Instruments

## Slide 20: TOSCA
Indirect Geometry Instruments
n
Spec
Water moderator
E = 0~600 meV
ΔE/E = 1%
(energy transfer)
Detectors only around:
40-55° (forward)
125-140° (back)

## Slide 21: IRIS
Indirect Geometry Instruments
Spec
Hydrogen moderator
E < 4 meV
ΔE ~ 18µeV (PG)
High flux
Detectors 25<2θ<160°

## Slide 22: OSIRIS
Indirect Geometry Instruments
Spec
Hydrogen moderator
E < 4 meV
ΔE ~ 25µeV (PG)
Very high flux
Detectors 11<2θ<148°

## Slide 23: Around the world
ISIS | TOSCA | IRIS/OSIRIS
SNS | VISION | BASIS
J-Parc |  | DNA
Indirect Geometry Instruments

## Slide 24
Questions so far?

## Slide 25
Phonons are quantised lattice vibrations
Can be treated as collective motions of particles (mass m) connected by springs with force constant C
Simplest case of a monatomic chain:
With solutions:
Giving a dispersion relation:
Phonons

## Slide 26
Phonons
0 0.2 0.4 0.6 0.8 1.0
q (π/a)
ħω
Transverse Acoustic Phonons
Longitudinal
Phonons
Phonons

## Slide 27
Phonons
Phonons
What does a INS phonon spectra look like?
See that there is much more intensity at high |Q| than low.

## Slide 28
The dynamical structure factor for phonon scattering is:
In a powder or polycrystalline sample, we have to average over all the directions of the momentum transfer Q.
At large |Q|>>|q| for a given |Q| the angular average is also approximately an average over a Brillouin zone so the term disappears and the . term can be replaced by the density of states Z(E), giving:
This is called the incoherent approximation.
Phonons
Methods of experimental physics: Neutron scattering Pt A by Sköld and Price, Ch 1
Phonon dynamic structure factor
Debye Waller factor
Polarization vector of mode d
Polarization factor

## Slide 29
Phonons
Phonons
Often though, the term is approximated as Q2, but this is strictly only valid for single-component systems.
But the take home message here is the neutron intensity of phonon scattering increases with increasing Q.

## Slide 30
Due to the magnetic dipolar interaction between the neutron moment and electronic spins.
Scattering function for magnetic neutron scattering is:
Magnetic Inelastic Scattering
Methods of experimental physics: Neutron scattering Pt A by Sköld and Price, Ch 1
M⊥ factor
Magnetic Form Factor
Magnetic form factor is highest at low Q:
Because the electronic spins have a finite extent so their Fourier Transform is concentrated at low Q.
For phonons, scattering is due to the neutron-nucleus interaction, and nuclei are point particles compared to atoms
Magnetic excitations are most intense at low Q, opposite to phonon scattering.

## Slide 31
Quantised collective precession of spins – small deviations from ordered magnetic state
Dispersive, can look like phonons
But, most intense at low Q.
Unlike X-rays, magnetic intensity for neutrons can be larger than lattice vibrations.
Spin waves
Can be modelled using linear spin wave theory with SpinW in later part of course.

## Slide 32
Transitions between localised electronic states with different Jz or Lz quantum number excited on a particular magnetic ion excited by neutrons.
Dispersionless, but follow form factor.
Will be covered on Day 10 practical.
Crystal Fields

## Slide 33
Questions so far?
(and 5 min break)

## Slide 34
MSlice Demonstration
MSlice Demonstration

## Slide 35
INS can be visualised using the scattering triangle.
In continuous sources (reactors), need to define both the incident and scattered neutron energy / wavevector (ki and kf ).
In time-of-flight INS, only need to define either ki or kf and use the ToF to infer the other.
ToF where ki is fixed is direct geometry.
ToF where kf is fixed is indirect geometry.
There are different kinematic trajectories for each case.
Summary

## Slide 36
Phonons are quantised lattice vibrations (collective motions of atoms).
Phonon INS intensity is larger at high |Q| (approximately proportional to |Q|2).
Magnons are quantised spin precessions in an ordered magnetic state.
Crystal field excitations are excitations between localised electronic states with different with different Jz or Lz quantum number.
Magnetic excitations (magnons and crystal fields) follow the magnetic form factor and have highest INS intensity at low |Q|.
Summary