## Slide 1
Linear Spin Wave Calculations with SpinW part II
Notes: 1

## Slide 2
Overview
Spin-spin correlation tensor
  Polarised neutron intensities
Twinned crystals
Simulated annealing and Monte Carlo calculations
  Magnetic structure refinement
  Calculating magnetisation, susceptibility

## Slide 3
Recap
tri = spinw;
tri.genlattice('lat_const', [4 4 6], 'angled', [90 90 120]);
tri.addatom('r', [0 0 0], 'S', 2, 'label', 'MCr3', 'color', 'gold');
tri.genmagstr('mode', 'helical', 'S', [1; 0; 0], ...
'n', [0 0 1], 'k', [1/3 1/3 0])
spec = tri.spinwave({[0,0,0], [1,1,1], [1,0,0] 200});
spec = sw_egrid(spec);
sw_plotspec(spec, 'dE', 0.1)
modQ = linspace(0,3,100);
spec = tri.powspec(modQ, 'nRand', 10000, 'Evect', linspace(0,4,200));
figure; sw_plotspec(spec)

## Slide 4
Spin-spin correlation function
spinwave returns a spectrum struct
Initially only has Sab – a 3x3xMxN array, M=# modes, N=# Q-pts.
Use sw_neutron to calculate interesting cross-sections.
sw_egrid internally calls sw_neutron to calculate Sperp – the component of S perpendicular to Q which is measured in unpolarised neutron scattering.

## Slide 5
Spin-spin correlation function
spinwave returns a spectrum struct
Initially only has Sab – a 3x3xMxN array, M=# modes, N=# Q-pts.
Use sw_neutron to calculate interesting cross-sections.
sw_egrid internally calls sw_neutron to calculate Sperp – the component of S perpendicular to Q which is measured in unpolarised neutron scattering.
But can use either sw_egrid or sw_neutron with the 'component' option to calculate other quantities.

## Slide 6
Spin-spin correlation function
Can calculate and plot:
  Individual components of Sαβ or their sum. E.g.
  Polarised neutron cross-sections – first have to run sw_neutron with the 'pol',true option and to define the horizontal scattering plane.
  This is because polarised cross-sections use the Blume-Maleyev coordinate system where x||Q, z is vertical and y⊥(x,z).
  Can specify the horizontal plane either by a u and v matrix (like Horace) – these are reciprocal lattice vectors. Or, can specify the direction of the plane normal in the SpinW Cartesian coordinate system: x||a, z⊥(a,b) and y⊥(x,z).
sw_plotspec(sw_egrid(spec, 'component', 'Sxx+Syy'), 'dE', 0.1)
spec = sw_neutron('pol', true, 'uv', {[1,0,0], [0,1,0]})
sw_plotspec(sw_egrid(spec, 'component', 'Pz'), 'dE', 0.1)
spec = sw_neutron('pol', true, 'n', [0,0,1])
sw_plotspec(sw_egrid(spec, 'component', 'Pz'), 'dE', 0.1)

## Slide 7
Spin-spin correlation function
Can calculate and plot:
  'Pa' – a=x,y,z – half polarized intensity with incident beam polarised along a certain direction
  'Pab' – a,b=x,y,z – xyz polarized intensity σαβ with incident and scattered beam polarized along the specified direction
  'Mab' – a,b=x,y,z – magnetisation component along the specified direction.
sw_plotspec(sw_egrid(spec, 'component', 'Pz'), 'dE', 0.1)
sw_plotspec(sw_egrid(spec, 'component', 'Pyy'), 'dE', 0.1)
sw_plotspec(sw_egrid(spec, 'component', 'Myz-Mzy'), 'dE', 0.1)

## Slide 8
System is iron-langasite Ba3NbFe3Si2O14. (SpinW tutorial 15)
Polarised neutron example
Loire et al., Phys. Rev. Lett., 106 207201 (2011)

## Slide 9
System is iron-langasite Ba3NbFe3Si2O14. (SpinW tutorial 15)
Polarised neutron example
Loire et al., Phys. Rev. Lett., 106 207201 (2011)

## Slide 10
System is iron-langasite Ba3NbFe3Si2O14. (SpinW tutorial 15)
Polarised neutron example
Loire et al., Phys. Rev. Lett., 106 207201 (2011)
banbSpec = banb.spinwave({[0 1 -1] [0 1 2] 500});
banbSpec = sw_neutron(banbSpec,'pol',true,'uv',{[0 1 0] [0 0 1]});
figure
banbSpec = sw_egrid(banbSpec,'component','Sperp', ...
'Evect',linspace(0,6,500));
sw_plotspec(banbSpec,'mode','color','dE',0.25,'axLim',[0 10]);
colormap(jet)

## Slide 11
System is iron-langasite Ba3NbFe3Si2O14. (SpinW tutorial 15)
Polarised neutron example
Loire et al., Phys. Rev. Lett., 106 207201 (2011)
banbSpec = banb.spinwave({[0 1 -1] [0 1 2] 500});
banbSpec = sw_neutron(banbSpec,'pol',true,'uv',{[0 1 0] [0 0 1]});
figure
banbSpec = sw_egrid(banbSpec,'component','-Myz+Mzy', ...
'Evect',linspace(0,6,500));
sw_plotspec(banbSpec,'mode','color','dE',0.25,'axLim',[-10 10],'imag',true);
colormap(makecolormap([0 0.5 0],[0.5 0.8 0.5],[0 0 0.5],81));

## Slide 12
Questions so far?

## Slide 13
Twinned Crystals
Spin-spin correlation tensor
  Polarised neutron intensities
Twinned crystals
Simulated annealing and Monte Carlo calculations
  Magnetic structure refinement
  Calculating magnetisation, susceptibility

## Slide 14
Twinned crystals can be handled by using addtwin:
Example for a cut integrating over energy, with a model of Pr(Ca,Sr)Mn2O7
Twinned Crystals
pcsmo.addtwin('axis', [0 0 1], 'phid', 90)
nQ = 101; Qhv = linspace(-2,2,nQ); Qkv = linspace(-2,2,nQ); Qlv = 0;
nE = 201; Ev = linspace(0,100,nE);
Ecut = [34 36];
[Qh, Qk, Ql] = ndgrid(Qhv,Qkv,Qlv);
spec = pcsmo.spinwave([Qh(:) Qk(:) Ql(:)]', 'sortMode', false, 'hermit', false);
spec = sw_egrid(spec,'component','Sperp','Evect',Ev);
spec = sw_instrument(spec,'dE',5);
spec3D = reshape(spec.swConv,nE-1,nQ,nQ);
Eidx = find(Ev>Ecut(1) & Ev<Ecut(2));
figure;
cut1 = squeeze(sum(spec3D(Eidx,:,:),1))/numel(Eidx)/(Ev(2)-Ev(1));
imagesc(Qhv/2,Qkv/2,cut1);
xlabel('Qh'); ylabel('Qk');

## Slide 15
Twinned crystals can be handled by using addtwin:
Example for a cut integrating over energy, with a model of Pr(Ca,Sr)Mn2O7
Twinned Crystals
pcsmo.addtwin('axis', [0 0 1], 'phid', 90)
nQ = 101; Qhv = linspace(-2,2,nQ); Qkv = linspace(-2,2,nQ); Qlv = 0;
nE = 201; Ev = linspace(0,100,nE);
Ecut = [34 36];
[Qh, Qk, Ql] = ndgrid(Qhv,Qkv,Qlv);
spec = pcsmo.spinwave([Qh(:) Qk(:) Ql(:)]', 'sortMode', false, 'hermit', false);
spec = sw_egrid(spec,'component','Sperp','Evect',Ev);
spec = sw_instrument(spec,'dE',5);
spec3D = reshape(spec.swConv,nE-1,nQ,nQ);
Eidx = find(Ev>Ecut(1) & Ev<Ecut(2));
figure;
cut1 = squeeze(sum(spec3D(Eidx,:,:),1))/numel(Eidx)/(Ev(2)-Ev(1));
imagesc(Qhv/2,Qkv/2,cut1);
xlabel('Qh'); ylabel('Qk');
Without twin calculation
Twin calculation

## Slide 16
Twinned crystals can be handled by using addtwin:
Example for a cut integrating over energy, with a model of Pr(Ca,Sr)Mn2O7
Twinned Crystals
pcsmo.addtwin('axis', [0 0 1], 'phid', 90)
nQ = 101; Qhv = linspace(-2,2,nQ); Qkv = linspace(-2,2,nQ); Qlv = 0;
nE = 201; Ev = linspace(0,100,nE);
Ecut = [34 36];
[Qh, Qk, Ql] = ndgrid(Qhv,Qkv,Qlv);
spec = pcsmo.spinwave([Qh(:) Qk(:) Ql(:)]', 'sortMode', false, 'hermit', false);
spec = sw_egrid(spec,'component','Sperp','Evect',Ev);
spec = sw_instrument(spec,'dE',5);
spec3D = reshape(spec.swConv,nE-1,nQ,nQ);
Eidx = find(Ev>Ecut(1) & Ev<Ecut(2));
figure;
cut1 = squeeze(sum(spec3D(Eidx,:,:),1))/numel(Eidx)/(Ev(2)-Ev(1));
imagesc(Qhv/2,Qkv/2,cut1);
xlabel('Qh'); ylabel('Qk');
Without twin calculation
Twin calculation

## Slide 17
Simulated Annealing
Spin-spin correlation tensor
  Polarised neutron intensities
Twinned crystals
Simulated annealing and Monte Carlo calculations
  Magnetic structure refinement
  Calculating magnetisation, susceptibility

## Slide 18
Simulated Annealing
SpinW has a routine for running a Monte Carlo simulated annealing calculation to:
  Optimise a magnetic structure
  Calculate physical properties (magnetisation, susceptibility, heat capacity)
Algorithm is:
  Create a large ensemble / box of random spins using nExt
  Partition this into non-interacting sublattices.
  Choose a starting simulated temperature initT
  Calculate the initial energy
  For each spin, choose a new random orientation
  Calculate the change in energy
  Apply the Metropolis criteria:
  Loop for nMC steps
  Lower the simulated temperature T by step
  determined by cool and loop until endT

## Slide 19
Uses the anneal method of the spinw object.
Simulated Annealing
tri = sw_model('triAF', [-4 16]);
% Removes units
tri.unit.kB = 1;
tri.unit.muB = 1;
tri.field([0 0 0]);
tri.anneal('verbosity',2, 'cool',@(T)(0.8*T), 'initT', 100, 'endT', 1e-2, ...
'nMC',1e3, 'nStat',0, 'random',true, 'nExt',[50 50 1], 'spinDim', 2);

## Slide 20
Uses the anneal method of the spinw object.
Simulated Annealing
tri = sw_model('triAF', [-4 16]);
% Removes units
tri.unit.kB = 1;
tri.unit.muB = 1;
tri.field([0 0 0]);
tri.anneal('verbosity',2, 'cool',@(T)(0.8*T), 'initT', 100, 'endT', 1e-2, ...
'nMC',1e3, 'nStat',0, 'random',true, 'nExt',[50 50 1], 'spinDim', 2);

## Slide 21
Uses the annealoop method to calculate physical properties.
Simulated Annealing
hChain = sw_model('chain', 2);
hChain.addmatrix('value', diag([0 0 -0.2]), 'label', 'A'); hChain.addaniso('A')
hChain.unit.kB = 1; hChain.unit.muB = 1;
hChain.anneal('verbosity',2, 'cool',@(T)(0.8*T), 'initT', 100, 'endT', 1e-2, ...
'nMC',1e3, 'nStat',0, 'random',true, 'nExt',[150 1 1]);
fieldSweep = [linspace(0,5,40) linspace(5,0,40)];
pStat = hChain.annealloop('x' ,fieldSweep, 'func',@(obj,x)obj.field([0 0 x]), ...
'nMC',2e4 ,'nStat',1e4, 'tid',2, 'fineT', 1e-2);
M = squeeze(sum(pStat.avgM,2))/hChain.nmagext;
figure; plot(pStat.x,M(3,:),'g.-')
xlabel('Magnetic Field (T)'); ylabel('Magnetic moment'); legend('M_z')

## Slide 22
Uses the annealoop method to calculate physical properties.
Simulated Annealing
hChain = sw_model('chain', 2);
hChain.addmatrix('value', diag([0 0 -0.2]), 'label', 'A'); hChain.addaniso('A')
hChain.unit.kB = 1; hChain.unit.muB = 1;
hChain.anneal('verbosity',2, 'cool',@(T)(0.8*T), 'initT', 100, 'endT', 1e-2, ...
'nMC',1e3, 'nStat',0, 'random',true, 'nExt',[150 1 1]);
fieldSweep = [linspace(0,5,40) linspace(5,0,40)];
pStat = hChain.annealloop('x' ,fieldSweep, 'func',@(obj,x)obj.field([0 0 x]), ...
'nMC',2e4 ,'nStat',1e4, 'tid',2, 'fineT', 1e-2);
M = squeeze(sum(pStat.avgM,2))/hChain.nmagext;
figure; plot(pStat.x,M(3,:),'g.-')
xlabel('Magnetic Field (T)'); ylabel('Magnetic moment'); legend('M_z')

## Slide 23
Questions so far?
(and 5 min break)

## Slide 24
SpinW Demonstration
SpinW Demonstration

## Slide 25
Spin-spin correlation functions
  How to calculate polarised neutron cross-sections
Twinned samples
Simulated Annealing Monte Carlo calculations
  How to calculate physical properties
Summary