## Slide 1: Measuring Phonons with Neutrons
D. J. Voneshen – Excitations training course
8/7/2021

## Slide 2: Contents
What and why phonons?
One phonon cross section
Measuring single crystals
Measuring powders
Incoherent approximation

## Slide 3: Why Phonons?
Not just background!
Lattice dynamics is important for
  Bonding
  Heat transfer
  Phase transitions
  Some superconductors

## Slide 4: Phonons an overview
We are going to do everything within the harmonic approximation.
So, forces on atom n if displaced in is

## Slide 5: Phonons an overview
We are going to do everything within the harmonic approximation.
So, forces on atom n if displaced in is
. This is a second order differential, if we try
and work through it

## Slide 6: Phonons, an overview
As we saw in the first practical, our maximum frequency is related to the spring constant and mass.
So strong bonds, high frequency.
Light isotopes also are at high energy.

## Slide 7: Phonons, an overview

## Slide 8: Now to neutrons!

## Slide 9: One phonon coherent scattering

## Slide 10: One phonon coherent scattering

## Slide 11: One phonon coherent scattering

## Slide 12: One phonon coherent scattering

## Slide 13: One phonon coherent scattering

## Slide 14: One phonon scattering-key points
Phonons are strongest when is parallel to direction of atomic motion.
Phonon intensity goes up with .
Phonons are weaker at high energy.
Strong Bragg reflections often have strong phonons around them.
Phonons can be stronger at high temperature (but care needed here).

## Slide 15: Measuring a longitudinal acoustic phonon
We want to measure a longitudinal phonon along 00L.
Which peak would be best to measure around?

## Slide 16: Measuring a longitudinal acoustic phonon
We want to measure a longitudinal phonon along 00L.
Which peak would be best to measure around?

## Slide 17: Measuring a transverse acoustic phonon
What about a transverse phonon along 00l?

## Slide 18: Measuring a transverse acoustic phonon
What about a transverse phonon along 00l?

## Slide 19: Exploiting , an example
We were looking for a phonon around 12 meV.
However, the background from the cryostat/mount was huge.
Rotate sample 90°. Suppresses, phonon but background unchanged

## Slide 20: Exploiting , an example
We were looking for a phonon around 12 meV.
However, the background from the cryostat/mount was huge.
Rotate sample 90°. Suppresses phonon but background unchanged

## Slide 21: Powders!
Good news, powder experiments are simpler!
Much simpler.
With them we can extract the neutron weighted phonon density of states.
But, going beyond that is hard.

## Slide 22: Powders, what are we doing?
We are averaging over a sphere at some .
So, for small values of we are covering just a few (or even 1) Brillouin zones.
But, for large we are covering many zones, essentially capturing everything in 1 shot.
This means for high we can no longer see the effect of and the signal is the same as incoherent scattering.

## Slide 23: Powders, what are we doing?
We are averaging over a sphere at some .
So, for small values of we are covering just a few (or even 1) Brillouin zones.
But, for large we are covering many zones, essentially capturing everything in 1 shot.
This means for high we can no longer see the effect of and the signal is the same as incoherent scattering.

## Slide 24: The neutron weighted phonon density of states
We normally correct the data for the effects of Bose statistics, and .
Then, in the incoherent approximation, the real Phonon Density of States (PDOS) is related to the PDOS we see via the above.
This means we cannot obtain the true PDOS for anything other than a monoatomic system.

## Slide 25: Beyond the harmonic approximation
This is where all the interesting stuff happens
But, it gets tricky fast.
Phonon-phonon scattering (broadening)
Multiphonon signals (signal above the top of the dispersion)

## Slide 26: Beyond the harmonic approximation

## Slide 27
@STFC_matters
Science and Technology Facilities Council
Science and Technology Facilities Council
Notes: The abstract pattern can be removed or repositioned if required. Be careful to ‘Send to Back’ so that it does not obscure any important information.